Remaining Fatigue Life — Sheave-Shaft Screening Estimate

FINAL ANSWER  41,872,316 cycles remaining

Calculation

mean tested life       = 44,872,500 cycles

accumulated service    = 3,000,184 cycles

remaining life         = 41,872,316 cycles

Input record

| Input | Value shown | Source resolution / limitation |
| --- | --- | --- |
| Constant-amplitude tests | 12 specimens | one synthetic batch; one stress range |
| Cycles to crack | 35,780,000–56,000,000 | recorded to nearest 10,000 cycles |
| Sample spread | SD 6,268,750 cycles | test-to-test variability |
| Accumulated service | 3,000,184 cycles | screening estimate |

Automated interpretation

Use the calculated value as the single remaining-life figure in the interim planning table.

No reporting range is required because the arithmetic returned one point estimate.

Model confidence: HIGH.

UNRESOLVED BASIS  This screening output does not quantify test scatter, specimen-to-component transfer, variable-amplitude loading, environment, inspection uncertainty, or the statistical basis for the displayed digits.